## Slide 1
Case Study 4 – The technical investigation of 8th-10th c statuettes from Indonesia
Home
MG 3625
MG 3816
MA 507
MG 18290
MG 3814 (Bangladesh)
8th-early 9th c
(Category 1)
1st half 9th c
(Category 2)
1st half 10th c
(category 3)
2nd half 9th c
(Category 2)
MG 2255
Late 9th c
(Category 2)
MG 3619
Main Questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 434
FIG 423
FIG 437
FIG 161
FIG 166
FIG 963
FIG 964

## Slide 2
Home
MG 3625
MG 3816
MA 507
MG 18290
MG 3814 (Bangladesh)
8th-early 9th c
(Category 1)
1st half 9th c
(Category 2)
1st half 10th c
(category 3)
2nd half 9th c
(Category 2)
MG 2255
Late 9th c
(Category 2)
MG 3619
Main Questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 434
FIG 423
FIG 437
FIG 161
FIG 166
FIG 963
FIG 964
Main questions

## Slide 3
Casting technique: lost- wax casts with numerous wax assemblies
Home
MG 3814
MG 18290
MG 3625
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 423
FIG 430
FIG 166

## Slide 4
Home
Casting technique: solid-cast figures
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 447
FIG 448

## Slide 5
Visual evidence of extensive cold work
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 423
FIG 425
FIG 166
FIG 167
FIG 166 zoom in

## Slide 6
Engraving, as suggested by Reflectance Transformation Imaging (RTI)
Home
MG 3822
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 191

## Slide 7
Metal punching confirmed by digital microscopy
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
Fig. 235
Fig. 236

## Slide 8
Metal engraving over wax preparatory drawing confirmed by digital microscopy
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 166 zoom in
FIG 169

## Slide 9
Home
Cavities filled with dense material
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 445

## Slide 10
Consecration deposits revealed from below
MG 18290
MG 3625
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 423
FIG 430
FIG 437
FIG 442

## Slide 11
Consecration deposits revealed by neutron radiography and tomography
Home
Nuetron radiographs
X-radiographs
MG 3625
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 443
FIG 444

## Slide 12
Home
Spinning of the raw neutron radiographies
Slicing the statue
Consecration deposits revealed by neutron radiography and tomography
MG 18290
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 449

## Slide 13
Home
Alloy composition
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions

## Slide 14
Home
Impurities in the metal
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions

## Slide 15
Home
Summary of findings – Consistent features of Indonesian production
Solid cast
Extensive wax working
Cavities sealed with liquid metal instead of hammered sheets
Unleaded tin bronzes with high levels of tin
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
FIG 447
FIG 448
FIG 166

## Slide 16
8th-early 9th
1st half 9th
2nd half 9th
Late 9th
1st half 10th
Summary of findings -Towards a chronological and stylistic serialization supported by metal composition
Median content of tin for each period
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions

## Slide 17
Summary of findings –Tin bronzes: Technical connections with South East Asia mainland
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions

## Slide 18
Summary of findings –Characterization of ritual offerings thanks to neutron tomography
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions

## Slide 19
Synopsis of technical parameters:
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
The Case Study is based on a technical study carried out by Mathilde Mechling in collaboration with David Bourgarit and Brice Vincent as part of her ongoing Ph.D. project on Indonesian bronze sculpture.
The examination and analyses were integrally carried out for free at the C2RMF as a service provided to French Museums, namely the Musée National des Arts Asiatiques - Guimet. Neutron tomography was also carried out for free at Reactor Orphée-Laboratoire Léon Brillouin, CEA-CNRS, France as a service for public research.r Main operating conditions are reported in Mechling et al 2019.
The approximate time required to carry out the whole study excluding publication may be estimated at more than 60 persons-day):
Day light & UV photography: Anne Maigret (C2RMF),
Digital microscopy Mathilde Mechling (PhD)& D Bourgarit + D Robcis (C2RMF)
X-ray radiography Elsa lambert (C2RMF)Neutron tomography Frédéric Ott (CNRS-CEA)
Bulk metal analysis by ICP-AES. Nathalie Gandolfo & D Bourgarit (C2RMF)
XRF : D Bourgarit (C2RMF)

## Slide 20
Further questions
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions
If comparative data from either similar objects or copper and tin deposits is evolved, will it be possible to investigate the provenance of the metal?
Is there physical evidence pointing conclusively to the use of either the direct or the indirect process to form the wax model?
Can the fabrication of the hosting cavity be further elucidated?
Can it be determined whether the statuettes were cast horizontally or vertically? Since horizontal casting is attested in South India, Sri Lanka and Tibet, is it a feature that might help to determine intercultural exchanges?
Can a comprehensive quantification of tool marks (depth and angle of the grooves) by digital microscopy yield interesting clues regarding know-hows and workshops?
Can the identification of ritualistic items serve as a means of tracing the regional exchange of materials and, if so, can it be done non-destructively avoiding the desecration of the religious image?

## Slide 21
Further Resources
Fontein J., Soekmono R. and Sedyawati E. 1971. Ancient Indonesian art of the Central and Eastern Javanese Periods. New York: Asia Society.
Fontein J., Soekmono R. and Sedyawati E. 1990. The sculpture of Indonesia. Washington, D.C.: The National Gallery of Art.
Le Bonheur, A. 1971. La sculpture indonésienne au Musée Guimet. Paris: Presses universitaires de France.
van Lohuizen-de Leeuw, J. 1984. Indo-Javanese metalwork. Stuttgart: Linden-Museum.
Lunsingh Scheurleer, P. and Klokke, M.J. (eds.) 1988. Divine bronze: Ancient Indonesian bronzes from AD 600 to 1600. Leiden: Brill.
Mechling, M., Vincent, B., Baptiste, P., and Bourgarit, D. Forthcoming (2019). « Indonesian bronze-casting tradition: Technical investigations on thirty-nine Indonesian bronze statues (7th-11th c.) from the Musée national des arts asiatiques—Guimet, Paris », Bulletin de l’Ecole Française d’Extrême Orient 104.
Home
Main questions
Fabrication technique
Synopsis of technical parameters
Further Resources
Cold working
Consecration deposit
Metal composition
Summary of findings
Further Questions